## Slide 1: Complex polymer interactions in azobenzene-based photoresponsive polymers
William S. Oates
Department of Mechanical Engineering
Florida A&M-Florida State University
Tallahassee, FL 32308
Acknowledgements: NSF CAREER, AFOSR, Tim White (AFRL), Yousuff Hussaini, Jonghoon Bin, Somayeh Mashayekhi, Sabah Chowdhury, Paul Miles
CMO-BIRS Mathematical Problems of Orientationally Ordered Soft Solids
Oaxaca, Mexico

## Slide 2: Motivation
Light activated adaptable structures
  Remote temporal and spatial shape control
  Shape memory actuation
Multi-physics coupling
  Influence of molecular scale photoisomerization & polymer network evolution on macroscale
  Unusual photostriction
Performance & efficiency
  Role of heat and polymer network on shape change
Cheng, L., et al., J. Appl. Phys. v. 112, p. 013513, 2012.
Oates, W., Bin, J., “Unifying Relations in Polymer Photomechanics,” SPIE Smart Structures and Materials, v. 943202, doi: 10.1117/12.2084344, 2015.
W. Oates and J. Bin, in Shape Memory Polymers for Aerospace Applications: Novel Synthesis, Modeling, Characterization and Design, eds. G. P. Tandon, A. McClung, and J. Baur, 2015.
h
h
h
Increasing cross-link density
Opposite photostriction in SRGs
Complex deformation from optical vortex beams

## Slide 3: Light-Matter Controlled Adaptive Structures
Polarized light control
Excitation wavelengths
A. Ambrosio, et al., Nat. Comm., 3:989, 2012.
Molecular evolution
Microstructure induced shape change

## Slide 4
Azo-polymers

## Slide 5: Outline
Light-matter modeling
  Multiaxial photomechanical predictions
Model validation
  Experimental characterization of heat and photopolymer viscoelasticity/plasticity
  Bayesian uncertainty analysis
Fractional derivatives (time permitting)
Concluding remarks

## Slide 6: Modeling Framework
Unifying Concepts in Photomechanics

## Slide 7
Lattice vibrations at long wavelength limit
Optic mode
Acoustic mode
M
m
Optic mode
Local motion
Acoustic mode
Macroscopic deformation
--- D. F. Nelson, Phys. Rev. A, v. 44(6), p. 3985, 1991

## Slide 8
Molecular Energy Transfer Continuum deformation
Azobenzene electronic structure
Non-affine polymer deformation
Total photomechanical strain
light
heat

## Slide 9: Polymer Chemistry
E1aP
P6a12
D. Bublitz et al., Appl. Phys. B, 70, 863-865, 2000.
Cheng, L., et al., J. Appl. Phys. v. 112, p. 013513, 2012.
Bian, S., et al., J. Appl. Phys. v. 86(8), p. 4498, 1999.

## Slide 10
Acoustic and optic mode decomposition
Light-matter interactions
Losses via entropy generation
Lagrangian Density Relations
10

## Slide 11
Balance Equations
Maxwell’s equations
Linear momentum
Electronic (optical mode) force balance
Dipole energy
Quadrupole energy
Photostrictive azo-polymer coupling

## Slide 12: Stationary Bending and Twisting
Finite element/finite difference simulations
Uniform, polarized light exposure
Qualitative correlation with data
Numerical domain—material & surrounding vacuum
Initial polydomain azobenzene microstructure
Microstructure evolution—exposed side
Bending from gradient of microstructure through thickness
Microstructure evolution—bottom side
h
Polarization direction

## Slide 13: Surface Deformation
Comparisons made with complex surface deformation
  Linear polarized light
  Circularly polarized light
  Vortex beams with different topological charge
Linearly polarized light
Viswanathan, et. al, J. Mater. Chem., 9:1941, 1999.
A. Ambrosio, et al., Nat. Comm., 3:989, 2012.
W. Oates and J. Bin, “Non-equilibrium thermodynamics and electromagnetics of azobenzene liquid crystal polymer networks” Shape Memory Polymers for Aerospace Applications: Novel Synthesis, Modeling, Characterization and Design, eds. G. P. Tandon, A. McClung, and J. Baur, DEStech Publications, Inc. pg. 183-225, 2016.
Bin, J., Oates, W., "A Unified Material Description for Light Induced Deformation in Azobenzene Polymers," Scientific Reports, v. 5(14654), pp. 1-12, 2015.
trans state

## Slide 14: Stationary Surface Deformation
Circularly polarized light
Vortex beams with different topological charge
Circularly polarized light
cis state
trans state
trans state

## Slide 15: Topological Charge Analysis
Model Predictions
Validation
=1
=2
=5
=10

## Slide 16: Modeling Summary
Chemical structure influence on photostriction
  Long azo-spacers—prolate deformation
  Short azo-spacers—oblate deformation
Photostrictive parameters

## Slide 17: Experimental Characterization
Thermal, viscoelasticity, liquid crystal microstructure evolution

## Slide 18: Material Compositions
Azobenzene 35% weight polyimide composition
Azobenzene 20% weight polyacrylate composition

## Slide 19: Rate Dependence/Shape Memory
Photochemical and photomechanical measurements
Light induced blocked stress
Compositions
  Azo-polyimide (below)
  Azo-polyacrylate (next slide)
Light source
Piezo actuator
Servo control
Specimen
Laser (488nm) excitation (E x)
Laser (488nm) excitation (E x)
Laser (488nm) excitation (E x)

## Slide 20: Pre-stress and Photostriction
E
E

## Slide 21: Constitutive Parameter Analysis
Gibbs energy function
Multi-physics coupling
  Thermomechanics
  Electronic structure (azo)
  Photostriction
  Thermal energy
  Viscoelasticity
Entropy generation
Mobility dependence on free volume via trace of internal stress

## Slide 22: Polymer Mobility
Viscoelasticity  energy barrier
  Viscosity of internal network (inverse mobility)
Free volume effects on energy barrier
Hypothesis:
Internal hydrostatic stress
Arrhenius relation

## Slide 23: Bayesian Parameter Estimation
Thermal, viscoelasticity, liquid crystal microstructure evolution

## Slide 24: Bayesian Uncertainty Analysis
Quotes:
  It’s tough to make predictions, especially about the future, Neils Bohr.
  What is not surrounded by uncertainty cannot be the truth, Richard Feynman.
Information processing
  Lack of informationuncertainty
  Bayes’ rule is the machinery used to process information from prior knowledge into a new belief (posterior probability distribution)
Prior Information
Information Provided by Model and Data
Updated Information
e

## Slide 25: Parameter Estimation & UQ
Bayesian uncertainty quantification
  Estimation of light-induced heat generation
  Photomechanics coupled to thermo-viscoelastic/plastic behavior
    Numerical implementation
      Bayes’ equation
      MCMC/DRAM* sampling method
    *Markov Chain Monte Carlo/Delayed Rejection Adaptive Metropolis
Prior Distribution
Likelihood
Normalization factor
Posterior Distribution

## Slide 26: Elastic Modulus Uncertainty
Conduct cyclic loading on polyimide films
Quasi-static loading rate, 65 mHz
Parameter estimation of elastic modulus

## Slide 27: Thermal Effects
Light energy converted to heat determined
Energy balance
Simplified form
Thermal time constant
Lightheat energy conversion

## Slide 28: Rate Dependent Stress
Propagation of error in stress predictions
  Parameter uncertainty propagated through posterior densities
Broad parameter space sampled over
  Thermoelastic, viscoelastic, photostriction parameter estimation

## Slide 29: Perpendicular Light Excitation

## Slide 30: Parameter Comparisons
 | Mean | Standard Deviation
 (ppm/°C) | -- | --
EQ (kPa) | 431 | 33.4
0Q | 9.43E-07 | 3.09E-07
y | 2.23E+05 | 1.75E04
d33 | 1.77 | 0.16
d31 | -4.45 | 0.56
A | 138.8 | 5.36
Laser excitation (E x)
 | Mean | Standard Deviation
 (ppm/°C) | 116 | 28.7
EQ (kPa) | 1281 | 128.3
0Q | 56.9 | 59.7
y | 2.04E+07 | 7.47E+05
d33 | 4.39 | 0.42
d31 | -0.027 | 0.025
A | -- | --
Laser excitation (E x)

## Slide 31: Fractional Derivatives
Dielectric Elastomers

## Slide 32: Fractional Derivatives
Caputo derivative of fractional order 
  Applicable to linear viscoelasticity
Grunwald-Letnikov of fractional order 
  Applicable to nonlinear viscoelasticity
1
0
Memory

## Slide 33: Fractional Derivative Theory
Second law dependent upon polymer network evolution
Entropy generation function, is
Fractional derivative takes the form
Internal fractional stress dependence becomes
Notes: --polymer stretch ratio, --internal degrees of freedom of polymer network motion

## Slide 34: Parameter Analysis
Fixed set of hyperelastic parameters
Effect of fractional derivative order 

## Slide 35: Statistical Analysis
Figure 2: Parameter chain – sampled values for fractional order, , and coefficient, .
Model validated on 3M VHB elastomer
Parameter Sampling
  simulations
  Converged posterior densities
Figure 1: Parameter posterior densities – sampled values for fractional order, , and coefficient, .
 | 25.5 | 
 | 40.6 | 
 | 40.0 | 
 | 38.9 | 
 | 25.5 | 
 | 40.6 | 
 | 40.0 | 
 | 38.9 | 
Table 1: Mean parameter values from sampling of fractional order viscoelastic model.

## Slide 36: Predictions—Integer Order
Predict stress at stretch rates not used for model calibration.
  Integer order
  Nonlinear viscoelastic
  Calibrated at
Optimal fit requires 104 change in time constant

## Slide 37: Predictions—Fractional Order
Predict stress at stretch rates not used for model calibration.
  Fractional order
  Nonlinear viscoelastic
  Calibrated at
Optimal fit requires small change in fractional order
 | 25.5 | 
 | 40.6 | 
 | 40.0 | 
 | 38.9 | 
 | 25.5 | 
 | 40.6 | 
 | 40.0 | 
 | 38.9 | 

## Slide 38: Summary
Polarized light control of polymer deformation
  Advantageous in temporal and spatially controlled adaptive structures
Key developments
  Identified differences in dipole (electric field) and quadrupole (electric field gradient) forces on photostriction
  Rate dependent viscoelastic and shape memory effects quantified using uncertainty analysis
  Superior prediction of viscoelasticity using fractional derivatives
On-going research
  Materials synthesis of several mesogens and polymer systems with up-conversion
  Material repeatability
    Cyclic loading and viscoelastic/plastic effects in presence/absence of light
  Technology transfer to flow control

## Slide 39: Thank You

## Slide 40
Balance Equations
Maxwell’s equations
Linear momentum
Electronic (optical mode) force balance
Non-affine polymer deformation
Dipole energy
Quadrupole energy
Photostrictive azo-polymer coupling
Non-affine polymer network coupling